## Slide 1
Power Point for Optoelectronics and Photonics: Principles and Practices
Second Edition
ISBN-10: 0133081753
Second Edition Version 1.05800 [30 March 2016]
A Complete Course in Power Point
Chapter 2

## Slide 2
Updates and
Corrected Slides
Class Demonstrations
Class Problems
Check author’s website
http://optoelectronics.usask.ca
Email errors and corrections to safa.kasap@yahoo.com

## Slide 3
Slides on Selected Topics on Optoelectronics
may be available at the author website
http://optoelectronics.usask.ca
Email errors and corrections to safa.kasap@yahoo.com

## Slide 4
This Power Point presentation is a copyrighted supplemental material to the textbook Optoelectronics and Photonics: Principles & Practices, Second Edition, S. O. Kasap, Pearson Education (USA), ISBN-10: 0132151499, ISBN-13: 9780132151498. © 2013 Pearson Education. Permission is given to instructors to use these Power Point slides in their lectures provided that the above book has been adopted as a primary required textbook for the course. Slides may be used in research seminars at research meetings, symposia and conferences provided that the author, book title, and copyright information are clearly displayed under each figure. It is unlawful to use the slides for teaching if the textbook is not a required primary book for the course. The slides cannot be distributed in any form whatsoever, especially on the internet, without the written permission of Pearson Education.
Copyright Information and Permission: Part I
Please report typos and errors directly to the author: safa.kasap@yahoo.com

## Slide 5
This Power Point presentation is a copyrighted supplemental material to the textbook Optoelectronics and Photonics: Principles & Practices, Second Edition, S. O. Kasap, Pearson Education (USA), ISBN-10: 0132151499, ISBN-13: 9780132151498. © 2013 Pearson Education. The slides cannot be distributed in any form whatsoever, electronically or in print form, without the written permission of Pearson Education. It is unlawful to post these slides, or part of a slide or slides, on the internet.
Copyright © 2013, 2001 by Pearson Education, Inc., Upper Saddle River, New Jersey, 07458. All rights reserved. Printed in the United States of America. This publication is protected by Copyright and permission should be obtained from the publisher prior to any prohibited reproduction, storage in a retrieval system, or transmission in any form or by any means, electronic, mechanical, photocopying, recording, or likewise. For information regarding permission(s), write to: Rights and Permissions Department.
Copyright Information and Permission: Part II
PEARSON

## Slide 6
Important Note
You may use color illustrations from this Power Point in your research-related seminars or research-related presentations at scientific or technical meetings, symposia or conferences provided that you fully cite the following reference under each figure
From: S.O. Kasap, Optoelectronics and Photonics: Principles and Practices, Second Edition, © 2013 Pearson Education, USA

## Slide 7
Chapter 2 Dielectric Waveguides and Optical Fibers
Charles Kao, Nobel Laureate (2009)
Courtesy of the Chinese University of Hong Kong

## Slide 8
“The introduction of optical fiber systems will revolutionize the communications network. The low-transmission loss and the large bandwidth capability of the fiber systems allow signals to be transmitted for establishing communications contacts over large distances with few or no provisions of intermediate amplification.”
[Charles K. Kao (one of the pioneers of glass fibers for optical communications) Optical Fiber Systems: Technology, Design, and Applications (McGraw-Hill Book Company, New York, USA, 1982), p. 1]
Dielectric Waveguides and Optical Fibers
Courtesy of the Chinese University of Hong Kong
Charles Kao at the naming ceremony of Minor Planet (3463) "Kaokuen" by Nanjing's Purple Mountain Observatory in July 1996. Charles Kao and his colleagues carried out the early experiments on optical fibers at the Standard Telecommunications Laboratories Ltd (the research center of Standard Telephones and Cables) at Harlow in the United Kingdom, during the 1960s. He shared the Nobel Prize in 2009 in Physics with Willard Boyle and George Smith for "groundbreaking achievements concerning the transmission of light in fibers for optical communication." In a milestone paper with George Hockam published in the IEE Proceedings in 1966 they predicted that the intrinsic losses of glass optical fibers could be much lower than 20 dB/km, which would allow their use in long distance telecommunications. Today, optical fibers are used not only in telecommunications but also in various other technologies such as instrumentation and sensing. From 1987 to his retirement in 1996, professor Kao was the Vice Chancellor of the Chinese University of Hong Kong.(Courtesy of the Chinese University of Hong Kong.)

## Slide 9
Light is guided along a water jet as demonstrated by Jean-Daniel Colladon. This illustration was published in La Nature, Revue des Sciences, in 1884 (p. 325). His first demonstration was around 1841. (Comptes Rendes, 15, 800-802, Oct. 24, 1842). A similar demonstration was done by John Tyndall for the Royal Institution in London in his 1854 lecture. Apparently, Michael Faraday had originally suggested the experiment to John Tyndall though Faraday himself probably learned about it either from another earlier demonstration or through Jean-Daniel Colladon's publication. Although John Tyndall is often credited with the original discovery of a water-jet guiding light, Tyndall, himself, does not make that claim but neither does he attribute it to someone else. (The fountain, courtesy of Conservatoire Numérique des Arts et Métiers, France; Colladon's portrait, courtesy of Musée d'histoire des sciences, Genève, Switzerland.)
Reference: Jeff Hecht, "Illuminating the Origin of Light Guiding," Optics & Photonics News, 10, 26, 1999 and his wonderful book The City of Light (Oxford University Press, 2004) describe the evolution of the optical fiber from the water jet experiments of Colladon and Tyndall to modern fibers with historical facts and references.
1841
Jean-Daniel Colladon and the Light Guiding in a Water Jet

## Slide 10
Narinder Singh Kapany
Narinder Singh Kapany was born in Punjab in India, studied at the Agra University and then obtained his PhD from the Imperial College of Science and Technology, University of London in 1955. He held a number of key-positions in both academia and industry, including a Regents Professor at the University of California, Berkeley, the University of California, Santa Cruz (UCSC), the Director of the Center for Innovation and Entrepreneurial Development at UCSC. He made significant contributions to optical glass fibers starting in 1950s, and essentially coined the term fiber optics in the 1960s. His book Fibre Optics: Principles and Applications, published in 1967, was the first in optical fibers. (Courtesy of Dr. Narinder S. Kapany)

## Slide 11
A Century and Half Later
Light has replaced copper in communications. Photons have replaced electrons.
Will “Photonics Engineering” replace Electronics Engineering?

## Slide 12: WAVELENGTH DIVISION MULTIPLEXING: WDM

## Slide 13
Planar Optical Waveguide
A planar dielectric waveguide has a central rectangular region of higher refractive index n1 than the surrounding region which has a refractive index n2. It is assumed that the waveguide is infinitely wide and the central region is of thickness 2a. It is illuminated at one end by a nearly monochromatic light source.

## Slide 14
Light waves zigzag along the guide. Is that really what happens?
Optical Waveguide

## Slide 15
A light ray traveling in the guide must interfere constructively with itself to propagate successfully. Otherwise destructive interference will destroy the wave. E is parallel to x. (l1 and k1 are the wavelength and the propagation constant inside the core medium n1 i.e. l1 = l/n1.)
Waves Inside the Core

## Slide 16
Two arbitrary waves 1 and 2 that are initially in phase must remain in phase after reflections. Otherwise the two will interfere destructively and cancel each other.
Waves Inside the Core

## Slide 17
k1 = kn1 = 2pn1/l,
Df(AC) = k1(AB + BC) - 2f = m(2p)
BC = d/cosq and AB = BCcos(2q)
AB + BC = BCcos(2q) + BC = BC[(2cos2q -1) + 1] = 2dcosq
k1[2dcosq] - 2f = m(2p)
Waveguide condition
Waveguide Condition
and
Modes
m = 0, 1, 2, 3 etc
Integer
“Mode number”

## Slide 18
Propagation constant along the guide
Transverse Propagation constant

## Slide 19
Waveguide Condition and Waveguide Modes
To get a propagating wave along a guide you must have constructive interference. All these rays interfere with each other. Only certain angles are allowed . Each allowed angle represents a mode of propagation.

## Slide 20
m = integer, n1 = core refractive index, qm is the incidence angle, 2a is the core thickness.
Minimum qm and maximum m must still satisfy TIR.
There are only a finite number of modes.
Propagation along the guide for a mode m is
Waveguide Condition

## Slide 21
Waveguide Condition and Modes
To get a propagating wave along a guide you must have constructive interference. All these rays interfere with each other. Only certain angles are allowed . Each allowed angle represents a mode of propagation.

## Slide 22
Modes in a Planar Waveguide
E(y,z,t) = Em(y)cos(wt - bmz)
Traveling wave along z
Field pattern along y
We can identify upward (A) and downward (B) traveling waves in the guide which interfere to set up a standing wave along y and a wave that is propagating along z. Rays 2 and 2 belong to the same wave front but 2 becomes reflected before 2. The interference of 1 and 2 determines the field at a height y from the guide center. The field E(y, z, t) at P can be written as

## Slide 23
m = integer, n1 = core refractive index, qm is the incidence angle, 2a is the core thickness.
Modes in a Planar Waveguide: Summary
E(y,z,t) = Em(y)cos(wt - bmz)
Traveling wave along z
Field pattern along y

## Slide 24
Left: The upward and downward traveling waves have equal but opposite wavevectors km and interfere to set up a standing electric field pattern across the guide. Right: The electric field pattern of the lowest mode traveling wave along the guide. This mode has m = 0 and the highest q. It is often referred to as the glazing incidence ray. It has the highest phase velocity along the guide
Mode Field Pattern

## Slide 25
The electric field patterns of the first three modes (m = 0, 1, 2) traveling wave along the guide. Notice different extents of field penetration into the cladding
Modes in a Planar Waveguide

## Slide 26
Intermode (Intermodal or Modal) Dispersion
Schematic illustration of light propagation in a slab dielectric waveguide. Light pulse entering the waveguide breaks up into various modes which then propagate at different group velocities down the guide. At the end of the guide, the modes combine to constitute the output light pulse which is broader than the input light pulse.

## Slide 27
TE and TM Modes
Possible modes can be classified in terms of (a) transverse electric field (TE) and (b) transverse magnetic field (TM). Plane of incidence is the paper.
B^ is along - x, so that B^ = -Bx
E^ is along x, so that E^ = Ex

## Slide 28
V-Number
All waveguides are characterized by a parameter called the V-number or normalized frequency
V < /2, m = 0 is the only possibility and only the fundamental mode (m = 0) propagates along the dielectric slab waveguide: a single mode planar waveguide.
= c for V = /2 is the cut-off wavelength, and above this wavelength, only one-mode, the fundamental mode will propagate.

## Slide 29
Example on Waveguide Modes
Consider a planar dielectric guide with a core thickness 20 mm, n1 = 1.455, n2 = 1.440, light wavelength of 900 nm. Find the modes
Waveguide condition
TIR phase change fm for TE mode
Waveguide condition
TE mode

## Slide 30
TE mode

## Slide 31
m | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
qm | 89.2° | 88.3° | 87.5° | 86.7° | 85.9° | 85.0° | 84.2° | 83.4° | 82.6° | 81.9°
dm (mm) | 0.691 | 0.702 | 0.722 | 0.751 | 0.793 | 0.866 | 0.970 | 1.15 | 1.57 | 3.83
Critical angle qc = arcsin(n2/n1) = 81.77°
Highest
mode
m = 0
Fundamental
mode
Mode m, incidence angle qm and penetration dm for a planar dielectric waveguide with d = 2a = 20 mm, n1 = 1.455, n2 = 1.440 (l = 900 nm)
Notes: 31

## Slide 32
Number of Modes M
Waveguide condition
One mode when V < /2
Multimode when V > /2

## Slide 33
Mode Field Width 2wo
Ecladding(y¢) = Ecladding(0)exp(-acladdingy¢)
Mode Field Width 2wo
Note: The MFW definition here is semiquantitive. A more rigorous approach needs to consider the optical power in the mode and how much of this penetrates the cladding. See optical fibers section.

## Slide 34
The slope of w vs.  is the group velocity vg
Waveguide Dispersion Curve

## Slide 35
The slope of w vs.  is the group velocity vg
Waveguide Dispersion Curve
Slope = Group Velocity
bm
w

## Slide 36: Mode Group Velocities from Dispersion Diagram
The group velocity vg vs. w for a planar dielectric guide with a core thickness (2a) = 20 mm, n1 = 1.455, n2 = 1.440. TE0, TE1 and TE4
Group velocity vs. frequency or wavelength behavior is not obvious. For the first few modes, a higher mode can travel faster than the fundamental.

## Slide 37: A Planar Dielectric Waveguide with Many Modes
The group velocity vg vs. w for a planar dielectric guide Core thickness (2a) = 20 mm, n1 = 1.455, n2 = 1.440
[Calculations by the author]
w
vg
0.5×1016
1.0×1016
1.5×1016
0
2.04
2.05
2.06
2.07
2.08
×108
c / n2
c / n1
(c/n1)sinqc = cn2/n12
m = 0
m = 10
m = 20
m = 30
m = 40
m = 60
TE1 wcutoff
Slower than fundamental
Not in the textbook

## Slide 38: Dispersion in the Planar Dielectric Waveguide with TE0 and TE1 (Near cut-off)
TE0
TE1
=
Broadened pulse
Output light pulse
Input light
pulse
w
vg
wcutoff
c / n2
c / n1
Operating frequency w1
vgmax
vgmin
vgmax  c/n2
vgmin  c/n1
Spread in arrival times
Dispersion
TE1
TE0
TE2
w1
w1
l1 = 2pc/w1
Not in the textbook

## Slide 39: A Planar Dielectric Waveguide with Many Modes
Multimode operation in which many modes propagate with different group velocities
vg vs. w for a planar dielectric guide with a core thickness (2a) = 20 mm, n1 = 1.455, n2 = 1.440 [Calculations by the author]
w
vg
0.5×1016
1.0×1016
1.5×1016
0
2.04
2.05
2.06
2.07
2.08
×108
c / n2
c / n1
(c/n1)sinqc = cn2/n12
m = 0
m = 25
m = 35
m = 45
m = 55
m = 65
wcutoff
Operating frequency
Range of group velocities for 65 modes
Not in the textbook

## Slide 40: Dispersion in the Planar Dielectric Waveguide with Many Modes Far from Cutoff
TEhighest
qc
qc
c/n1
(c/n1)sinqc
c/n1
(Since n1 and n2 are only slightly different.)
w
vg
c / n1
(c/n1)sinqc
Operating frequency
Range of group velocities for 65 modes
c / n2
Not in the textbook

## Slide 41: Dispersion in the Planar Dielectric Waveguide Many Modes
TEhighest
qc
=
Broadened pulse
Output
pulse
Very short input pulse
w2
w2
qc
TE0
Dt
Not in the textbook
(Since n1/n2  1)

## Slide 42: How can a higher mode such as TE1 or TE2 travel faster than the fundamental near cut-off?
Not in the textbook
The mode TE1 penetrates into the cladding where its velocity is higher than in the core. If penetration is large, as near cut-off, TE1 group velocity along the guide can exceed that of TE0.
qc
Penetration depth dm
Incidence angle qi
TE1 near cut-off
Fundamental mode
Notes: 42

## Slide 43
The electric field of TE0 mode extends more into the cladding as the wavelength increases. As more of the field is carried by the cladding, the group velocity increases.
Group Velocity and Wavelength: Fundamental Mode

## Slide 44
Optical Fibers
The step index optical fiber. The central region, the core, has greater refractive index than the outer region, the cladding. The fiber has cylindrical symmetry. The coordinates r, f, z are used to represent any point P in the fiber. Cladding is normally much thicker than shown.

## Slide 45
Meridional ray enters the fiber through the fiber axis and hence also crosses the fiber axis on each reflection as it zigzags down the fiber. It travels in a plane that contains the fiber axis.
Skew ray enters the fiber off the fiber axis and zigzags down the fiber without crossing the axis

## Slide 46: Modes LPlm
Weakly guiding modes in fibers
 << 1 weakly guiding fibers
ELP = Elm(r,) expj(wt - blmz)
Traveling wave
Field
Pattern
E and B are 90o to each other and z

## Slide 47
Fundamental Mode is the LP01 mode: l = 0 and m = 1
The electric field distribution of the fundamental mode, LP01, in the transverse plane to the fiber axis z. The light intensity is greatest at the center of the fiber

## Slide 48
The electric field distribution of the fundamental mode in the transverse plane to the fiber axis z. The light intensity is greatest at the center of the fiber. Intensity patterns in LP01, LP11 and LP21 modes. (a) The field in the fundamental mode. (b)-(d) Indicative light intensity distributions in three modes, LP01, LP11 and LP21.

## Slide 49: LPlm
m = number of maxima along r starting from the core center. Determines the reflection angle q
2l = number of maxima around a circumference
l - radial mode number
l - extent of helical propagation, i.e. the amount of skew ray contribution to the mode.
ELP = Elm(r,) expj(wt - blmz)

## Slide 50
Optical Fiber Parameters
n = (n1 + n2)/2 = average refractive index
= normalized index difference
(n1n2)/n1  (n12n22)/2n12
V-number
V < 2.405 only 1 mode exists. Fundamental mode
V < 2.405 or > c Single mode fiber
V > 2.405 Multimode fiber
Number of modes

## Slide 51
Modes in an Optical Fiber
Normalized propagation constant
k = 2p/l
Normalized propagation constant b vs. V-number for a step-index fiber for various LP modes
( 1.5 < V < 2.5)

## Slide 52
Modes in an Optical Fiber
Normalized propagation constant can also be defined as
k = 2p/l
Normalized propagation constant b vs. V-number for a step-index fiber for various LP modes
( 1.5 < V < 2.5)

## Slide 53
Group Velocity and Group Delay
Consider a single mode fiber with core and cladding indices of 1.4480 and 1.4400, core radius of 3 mm, operating at 1.5 mm. What are the group velocity and group delay at this wavelength?
1.5 < V < 2.5
b = n2k[1 + bD]
k = 2p/l = 4,188,790 m-1 and w = 2pc/l = 1.255757×1015 rad s-1
V = (2a/l)(n12 - n22 )1/2 = 1.910088
Increase wavelength by 0.1% and recalculate. Values in the table
b = 0.3860859, and b = 6.044796×106 m-1.

## Slide 54
Group Velocity and Group Delay
The group delay tg over 1 km is 4.83 ms
Calculation  | V | k (m-1) | w (rad s-1) | b | b (m-1)
l = 1.500000 mm | 1.910088 | 4188790 | 1.255757×1015 | 0.3860859 | 6.044818×106
l¢ = 1.50150 mm | 1.908180 | 4184606 | 1.254503×1015 | 0.3854382 | 6.038757×106

## Slide 55
Mode Field Diameter (2w)
Gaussian
Gaussian
Intensity  vg×E(r)2
Note: Maximum set arbitrarily to 1

## Slide 56
Mode Field Diameter
0.8 < V < 2.5
2w  (2a)(2.6/V)
1.6 < V < 2.4
Marcuse MFD Equation
Intensity  vg×E(r)2
Note: Maximum set arbitrarily to 1
2w = Mode Field Diameter (MFD)

## Slide 57
Correction note p113
Applies to print version only; e-version is correct
Insert this 2 in Equation (2.3.7)
Insert this 2 as superscript on e in Figure 2.16

## Slide 58
Fraction of optical power within MFD
=
Area of a circular thin strip (annulus) with radius r is 2prdr. Power passing through this strip is proportional to
E(r)2(2pr)dr
Intensity  vg×E(r)2
and
Mode Field Diameter (2w)
Not in the textbook

## Slide 59
86% of total power
Fraction of optical power within MFD
= 86 %
This is the same as the fraction of optical power within a radius w from the axis of a Gaussian beam (See Chapter 1)
Mode Field Diameter (2w)

## Slide 60
Example: A multimode fiber
Calculate the number of allowed modes in a multimode step index fiber which has a core of refractive index of 1.468 and diameter 100 m, and a cladding of refractive index of 1.447 if the source wavelength is 850 nm.
Solution
Substitute, a = 50 m,  = 0.850 m, n1 = 1.468, n2 = 1.447 into the expression for the V-number,
V = (2a/)(n12n22)1/2 = (250/0.850)(1.46821.4472)1/2
= 91.44.
Since V >> 2.405, the number of modes is
M  V2/2 = (91.44)2/2 = 4181
which is large.

## Slide 61
Example: A single mode fiber
What should be the core radius of a single mode fiber which has a core of n1 = 1.4680, cladding of n2 = 1.447 and it is to be used with a source wavelength of 1.3 m?
Solution
For single mode propagation, V  2.405. We need,
V = (2a/)(n12n22)1/2 2.405
or
[2a/(1.3 m)](1.46821.4472)1/2  2.405
which gives a  2.01 m.
Rather thin for easy coupling of the fiber to a light source or to another fiber; a is comparable to l which means that the geometric ray picture, strictly, cannot be used to describe light propagation.

## Slide 62
Example: Single mode cut-off wavelength
Calculate the cut-off wavelength for single mode operation for a fiber that has a core with diameter of 8.2 mm, a refractive index of 1.4532, and a cladding of refractive index of 1.4485. What is the V-number and the mode field diameter (MFD) for operation at l = 1.31 mm?
Solution
For single mode operation,
V = (2a/)(n12n22 )1/2 2.405
Substituting for a, n1 and n2 and rearranging we get,
l > [2(4.1 mm)(1.45322 - 1.44852)1/2]/2.405 = 1.251 mm
Wavelengths shorter than 1.251 m give multimode propagation.
At  = 1.31 m,
V = 2p[(4.1 mm)/(1.31 mm)](1.45322 - 1.44852)1/2 = 2.30
Mode field diameter MFD

## Slide 63
Solution (continued)
Mode field diameter MFD from the Marcuse Equation is
2w = 9.30 mm
2w = (2a)(2.6/V) = 2(4.1)(2.6/2.30) = 9.28 mm
2w = 2a[(V+1)/V] = 11.8 mm
This is for a planar waveguide, and the definition is different than that for an optical fiber
86% of total power is within this diameter

## Slide 64
Numerical Aperture NA
2max = total acceptance angle
NA is an important factor in light launching designs into the optical fiber.
Maximum acceptance angle amax is that which just gives total internal reflection at the core-cladding interface, i.e. when a = amax then q = qc. Rays with a > amax (e.g. ray B) become refracted and penetrate the cladding and are eventually lost.

## Slide 65
Example: A multimode fiber and total acceptance angle
A step index fiber has a core diameter of 100 m and a refractive index of 1.480. The cladding has a refractive index of 1.460. Calculate the numerical aperture of the fiber, acceptance angle from air, and the number of modes sustained when the source wavelength is 850 nm.
Solution
The numerical aperture is
NA = (n12n22)1/2 = (1.48021.4602)1/2 = 0.2425 or 24.3%
From, sinmax = NA/no = 0.2425/1
Acceptance angle max = 14
Total acceptance angle 2max = 28
V-number in terms of the numerical aperture can be written as,
V = (2a/)NA = [(250 mm)/(0.85 mm)](0.2425) = 89.62
The number of modes, M  V2/2 = 4016
Normalized refractive index
D = (n1n2) / n1 = 0.0135 or 1.35%

## Slide 66
Example: A single mode fiber and cut-off wavelength
A typical single mode optical fiber has a core of diameter 8 m and a refractive index of 1.460. The normalized index difference is 0.3%. The cladding diameter is 125 m. Calculate the numerical aperture and the total acceptance angle of the fiber. What is the single mode cut-off frequency c of the fiber?
Solution
The numerical aperture
NA = (n12n22)1/2 = [(n1 + n2)(n1n2)]1/2
Substituting (n1n2) = n1 and (n1 + n2)  2n1, we get
NA  [(2n1)(n1)]1/2 = n1(2)1/2 = 1.46(20.003)1/2 = 0.113 or 11.3 %
The acceptance angle is given by
sinmax = NA/no = 0.113/1 or max = 6.5°, and 2max = 13°
The condition for single mode propagation is V  2.405. At cut-off,
V = (2a/c)(n12n22 )1/2 =2.405
 c = [2aNA]/2.405 = [(2)(4 m)(0.113)]/2.405 = 1.18 m
Wavelengths shorter than 1.18 m will result in multimode operation.

## Slide 67
Dispersion = Spread of Information
Intermode (Intermodal) Dispersion: Multimode fibers only
Material Dispersion Group velocity depends on Ng and hence on l
Waveguide Dispersion Group velocity depends on waveguide structure
Chromatic Dispersion Material dispersion + Waveguide Dispersion
Polarization Dispersion
Profile Dispersion Like material and waveguide dispersion. Add all 3 Material + Waveguide + Profile
Self phase modulation dispersion

## Slide 68
Intermode Dispersion (MMF)
Group Delay  = L / vg
(Since n1 and n2 are only slightly different)

## Slide 69
Intermode Dispersion (MMF)
Dt/L  - 50 ns / km
Depends on length!
qc
qc
TE0
TEhighest

## Slide 70
Intramode Dispersion (SMF)
Group Delay  = L / vg
Group velocity vg depends on
Refractive index = n(l) Material Dispersion
V-number = V(l) Waveguide Dispersion
 = (n1  n2)/n1 = (l) Profile Dispersion
Dispersion in the fundamental mode

## Slide 71
Intramode Dispersion (SMF)
Chromatic dispersion in the fundamental mode
l1
vg1
vg2
Dl = l2 - l1
l2
tg1
tg2
t
Dl
d(t)
Dt
Dt = tg2 - tg1
Dispersion
Chromatic spread
Definition of Dispersion Coefficient
OR
Output pulse dispersed

## Slide 72
Material Dispersion
Emitter emits a spectrum ∆l of wavelengths.
Waves in the guide with different free space wavelengths travel at different group velocities due to the wavelength dependence of n1. The waves arrive at the end of the fiber at different times and hence result in a broadened output pulse.
Dm = Material dispersion coefficient, ps nm-1 km-1

## Slide 73
Material Dispersion
Dm = Material dispersion coefficient, ps nm-1 km-1
vg = c / Ng
Depends on the wavelength
Group velocity

## Slide 74
Wave guide dispersion
b hence b depend on V and hence on l
Normalized propagation constant
k = 2p/l

## Slide 75
Waveguide Dispersion
Waveguide dispersion The group velocity vg(01) of the fundamental mode depends on the V-number, which itself depends on the source wavelength  even if n1 and n2 were constant. Even if n1 and n2 were wavelength independent (no material dispersion), we will still have waveguide dispersion by virtue of vg(01) depending on V and V depending inversely on . Waveguide dispersion arises as a result of the guiding properties of the waveguide which imposes a nonlinear  vs. lm relationship.
Dw = waveguide dispersion coefficient
Dw depends on the waveguide structure, ps nm-1 km-1

## Slide 76
Chromatic Dispersion
Material dispersion coefficient (Dm) for the core material (taken as SiO2), waveguide dispersion coefficient (Dw) (a = 4.2 mm) and the total or chromatic dispersion coefficient Dch (= Dm + Dw) as a function of free space wavelength, l
Chromatic = Material + Waveguide

## Slide 77
What do Negative and Positive Dm mean?
l1
1
2
l2
t
l1
vg1
vg2
l2
t
Dl = l2 - l1
1
2
l1
l2
Positive Dm
Ng2 > Ng1
Dt = Positive
t
l1
vg1
vg2
l2
t
Negative Dm
Ng2 < Ng1
Dt = Negative
Negative Dm
Positive Dm
Dm
Silica glass
Dt
Ng

## Slide 78
Waveguide Dimension and Chromatic Dispersion
Waveguide dispersion depends on the guide properties

## Slide 79
Profile Dispersion
Group velocity vg(01) of the fundamental mode depends on D, refractive index difference.
D may not be constant over a range of wavelengths: D = D()
Dp = Profile dispersion coefficient
Dp < 0.1 ps nm-1 km-1
Can generally be ignored
NOTE
Total intramode (chromatic) dispersion coefficient Dch
Dch = Dm + Dw + Dp
where Dm, Dw, Dp are material, waveguide and profile dispersion coefficients respectively

## Slide 80
Chromatic Dispersion
Dch = Dm + Dw + Dp
S0 = Chromatic dispersion slope at l0
Chromatic dispersion is zero at l = l0

## Slide 81
Is dispersion really zero at l0?
The cause of Dt is the wavelength spread Dl at the input
Dt = f(Dl)
= 0
Dl for multimode laser diode

## Slide 82
Polarization Dispersion
n different in different directions due to induced strains in fiber in manufacturing, handling and cabling. n/n < 10-6
DPMD = Polarization dispersion coefficient
Typically DPMD = 0.1 - 0.5 ps km-1/2

## Slide 83
Self-Phase Modulation Dispersion : Nonlinear Effect
At sufficiently high light intensities, the refractive index of glass n is
n = n + CI
where C is a constant and I is the light intensity. The intensity of light modulates its own phase.
What is the optical power that will give Dt/L  0.1 ps km-1?
Take C = 10-14 cm2 W-1
 I  (c/C)(Dt/L) = 36 W cm-2
or Dn  310-6
Given 2a  10 m, A  7.8510-7 cm2
Optical power  2.35 W in the core
In many cases, this dispersion will be less than other dispersion mechanisms

## Slide 84
Nonzero Dispersion Shifted Fiber
For Wavelength Division Multiplexing (WDM) avoid 4 wave mixing: cross talk.
We need dispersion not zero but very small in Er-amplifer band (1525-1620 nm)
Dch = 0.1 - 6 ps nm-1 km-1.
Nonzero dispersion shifted fibers
Various fibers named after their dispersion characteristics. The range 1500 - 1600 nm is only approximate and depends on the particular application of the fiber.

## Slide 85
Dispersion Flattened Fiber
Dispersion flattened fiber example. The material dispersion coefficient (Dm) for the core material and waveguide dispersion coefficient (Dw) for the doubly clad fiber result in a flattened small chromatic dispersion between l1 and l2.

## Slide 86
Nonzero Dispersion Shifted Fiber: More Examples
Nonzero dispersion shifted fiber (Corning)
Fiber with flattened dispersion slope (schematic)
0.6%
0.4%

## Slide 87: Commercial Fibers for Optical Communications
Fiber | Dch ps nm-1 km-1 | S0 ps nm-2 km-1 | DPMD ps km-1/2 | Some attributes
Standard single mode, ITU-T G.652 | 17 (1550 nm) | ≤ 0.093 | < 0.5 (cabled) | Dch = 0 at l0  1312 nm, MFD = 8.6 - 9.5 mm at 1310 nm. lc ≤1260 nm.
Non-zero dispersion shifted fiber, ITU-T G.655 | 0.1 - 6 (1530 nm) | < 0.05 at 1550 nm | < 0.5 (cabled) | For 1500 - 1600 nm range. WDM application MFD = 8 - 11 mm.
Non-zero dispersion shifted fiber, ITU-T G.656 | 2 - 14 | < 0.045 at 1550 nm | < 0.20 (cabled) | For 1460 - 1625 nm range. DWDM application. MFD = 7 - 11 mm (at 1550 nm). Positive Dch. lc <1310 nm
Corning SMF28e+ (Standard SMF) | 18 (1550 nm) | 0.088 | < 0.1 | Satisfies G.652. l0  1317 nm, MFD = 9.2 mm (at 1310 nm), 10.4 mm (at 1550 nm); lc ≤ 1260 nm.
OFS TrueWave RS Fiber | 2.6 - 8.9 | 0.045 | 0.02 | Satisfies G.655. Optimized for 1530 nm - 1625nm. MFD = 8.4 mm (at 1550 nm); lc ≤1260 nm.
OFS REACH Fiber | 5.5 -8.9 | 0.045 | 0.02 | Higher performance than G.655 specification. Satisfies G.656. For DWDM from 1460 to 1625 nm. l0 ≤ 1405 nm. MFD = 8.6 mm (at 1550 nm)

## Slide 88
Single Mode Fibers: Selected Examples

## Slide 89
Dispersion Compensation
Total dispersion = DtLt + DcLc = (10 ps nm-1 km-1)(1000 km) +
(100 ps nm-1 km-1)(80 km)
= 2000 ps/nm for 1080 km
Deffective = 1.9 ps nm-1 km-1

## Slide 90
Dispersion Compensation
Dispersion D vs. wavelength characteristics involved in dispersion compensation. Inverse dispersion fiber enables the dispersion to be reduced and maintained flat over the communication wavelengths.

## Slide 91
Dispersion Compensation and Management
Compensating fiber has higher attenuation. Doped core. Need shorter length
More susceptible to nonlinear effects. Use at the receiver end.
Different cross sections. Splicing/coupling losses.
Compensation depends on the temperature.
Manufacturers provide transmission fiber spliced to inverse dispersion fiber for a well defined D vs. l

## Slide 92
Dispersion and Maximum Bit Rate
Return-to-zero (RTZ) bit rate or data rate.
Nonreturn to zero (NRZ) bit rate = 2 RTZ bitrate

## Slide 93: NRZ and RTZ

## Slide 94
Maximum Bit Rate B
A Gaussian output light pulse and some tolerable intersymbol interference between two consecutive output light pulses (y-axis in relative units). At time t = s from the pulse center, the relative magnitude is e-1/2 = 0.607 and full width root mean square (rms) spread is Dtrms = 2s. (The RTZ case)

## Slide 95
Dispersion and Maximum Bit Rate
Maximum Bit Rate
Dispersion
Bit Rate × Distance is
inversely proportional to dispersion
inversely proportional to line width of laser
(so, we need single frequency lasers!)

## Slide 96
Dispersion and Maximum Bit Rate
Maximum Bit Rate

## Slide 97
Optical Bandwidth
An optical fiber link for transmitting analog signals and the effect of dispersion in the fiber on the bandwidth, fop.

## Slide 98: Pulse Shape and Maximum Bit Rate

## Slide 99
Example: Bit rate and dispersion
Consider an optical fiber with a chromatic dispersion coefficient 8 ps km-1 nm-1 at an operating wavelength of 1.5 m. Calculate the bit rate distance product (BL), and the optical and electrical bandwidths for a 10 km fiber if a laser diode source with a FWHP linewidth 1/2 of 2 nm is used.
Solution
For FWHP dispersion,
1/2/L = |Dch|1/2 = (8 ps nm-1 km-1)(2 nm) = 16 ps km-1
Assuming a Gaussian light pulse shape, the RTZ bit rate  distance product (BL) is
BL = 0.59L/t1/2 = 0.59/(16 ps km-1) = 36.9 Gb s-1 km
The optical and electrical bandwidths for a 10 km fiber are
fop = 0.75B = 0.75(36.9 Gb s-1 km) / (10 km) = 2.8 GHz
fel = 0.70fop = 1.9 GHz

## Slide 100
Graded Index (GRIN) Fiber
Multimode step index fiber. Ray paths are different so that rays arrive at different times.
Graded index fiber. Ray paths are different but so are the velocities along the paths so that all the rays arrive at the same time.

## Slide 101
A ray in thinly stratifed medium becomes refracted as it passes from one layer to the next upper layer with lower n and eventually its angle satisfies TIR.
In a medium where n decreases continuously the path of the ray bends continuously.
Graded Index (GRIN) Fiber

## Slide 102
Graded Index (GRIN) Fiber
The refractive index profile can generally be described by a power law with an index  called the profile index (or the coefficient of index grating) so that,
n = n1[12(r/a)]1/2 ; r < a,
n = n2 ; r ≥ a
Minimum intermodal dispersion
Minimum intermodal dispersion

## Slide 103
Graded Index (GRIN) Fiber
Minimum intermodal dispersion
Minimum intermodal dispersion
Profile dispersion parameter

## Slide 104
Graded Index (GRIN) Fiber
Effective numerical aperture for GRIN fibers
Number of modes in a graded index fiber

## Slide 105
Table 2.5
Graded index multimode fibers
d = core diameter (mm), D = cladding diameter (mm). Typical properties at 850 nm. VCSEL is a vertical cavity surface emitting laser. a is attenuation along the fiber. OM1, OM3 and OM4 are fiber standards for LAN data links (ethernet). a are reported typical attenuation values. 10G and 40G networks represent data rates of 10 Gb s-1 and 40 Gb s-1 and correspond to 10 GbE (Gigabit Ethernet) and 40 GbE systems.

## Slide 106: Example: Dispersion in a GRIN Fiber and Bit Rate
Graded index fiber. Diameter of 50 mm and a refractive index of n1 = 1.4750, D = 0.010.
The fiber is used in LANs at 850 nm with a vertical cavity surface emitting laser (VCSEL) that has very a narrow linewidth that is about 0.4 nm (FWHM). Assume that the chromatic dispersion at 850 nm is -100 ps nm-1 km-1 as shown in Table 2.5. Assume the fiber has been optimized at 850 nm, and find the minimum rms dispersion. How many modes are there? What would be the upper limit on its bandwidth? What would be the bandwidth in practice?
Solution
Given D and n1, we can find n2 from
D = 0.01 = (n1 - n2)/n1 = (1.4750 - n2)/1.4750.
n2 = 1.4603.
The V-number is then
V = [(2p)(25 mm)/(0.850 mm)(1.47502-1.46032)1/2 = 38.39
For the number of modes we can simply take g = 2 and use
M = (V2/4) = (38.392/4) = 368 modes
The lowest intermodal dispersion for a profile optimized graded index fiber for a 1 km of fiber, L = 1 km, is

## Slide 107: Example: Dispersion in a GRIN Fiber and Bit Rate
Solution continued
= 14.20×10-15 s m-1 or 14.20 ps km-1
Assuming a triangular output light pulse and the relationship between s and t1/2 given in Table 2.4, the intermodal spread tintermode (FWHM) in the group delay over 1 km is
tintermode = (61/2)sintermode = (2.45)(14.20 ps) = 34.8 ps
We also need the material dispersion at the operating wavelength over 1 km, which makes up the intramodal dispersion tintramode (FWHM)
tintramode = L|Dch| l1/2 = (1 km)(-100 ps nm-1 km-1)(0.40 nm) = 40.0 ps
t = 53.0 ps

## Slide 108: Example: Dispersion in a GRIN Fiber and Bit Rate
Solution continued
= 11.5 Gb s-1
Optical bandwidth fop = 0.99B = 11.4 GHz
This is the upper limit since we assumed that the graded index fiber is perfectly optimized with sintermode being minimum. Small deviations around the optimum g cause large increases in sintermode, which would sharply reduce the bandwidth.

## Slide 109: Example: Dispersion in a GRIN Fiber and Bit Rate
Solution continued
If this were a multimode step-index fiber with the same n1 and n2, then the full dispersion (total spread) would roughly be
= 4.92×10-11 s m-1 or 49.2 ns km-1
To calculate the BL we use sintermode  0.29Dt
= 17.5 Mb s-1 km
LANs now use graded index MMFs, and the step index MMFs are used mainly in low speed instrumentation

## Slide 110
Example: Dispersion in a graded-index fiber and bit rate
Consider a graded index fiber whose core has a diameter of 50 m and a refractive index of n1 = 1.480. The cladding has n2 = 1.460. If this fiber is used at 1.30 m with a laser diode that has very a narrow linewidth what will be the bit rate  distance product? Evaluate the BL product if this were a multimode step index fiber.
Solution
The normalized refractive index difference  = (n1n2)/n1 = (1.481.46)/1.48 = 0.0135. Dispersion for 1 km of fiber is
intermode/L = n1D2/[(20)(31/2)c] = 2.610-14 s m-1 or 0.026 ns km-1.
BL = 0.25/sintermode = 9.6 Gb s-1 km
We have ignored any material dispersion and, further, we assumed the index variation to perfectly follow the optimal profile which means that in practice BL will be worse. (For example, a 15% variation in  from the optimal value can result in intermode and hence BL that are more than 10 times worse.)
If this were a multimode step-index fiber with the same n1 and n2, then the full dispersion (total spread) would roughly be 6.6710-11 s m-1 or 66.7 ns km-1 and BL = 12.9 Mb s-1 km
Note: Over long distances, the bit rate  distance product is not constant for multimode fibers and typically B  L where  is an index between 0.5 and 1. The reason is that, due to various fiber imperfections, there is mode mixing which reduces the extent of spreading.

## Slide 111
Example: Combining intermodal and intramodal dispersions
Consider a graded index fiber with a core diameter of 30 m and a refractive index of 1.474 at the center of the core and a cladding refractive index of 1.453. Suppose that we use a laser diode emitter with a spectral linewidth of 3 nm to transmit along this fiber at a wavelength of 1300 nm. Calculate, the total dispersion and estimate the bit-rate  distance product of the fiber. The material dispersion coefficient Dm at 1300 nm is 7.5 ps nm-1 km-1.
Solution
The normalized refractive index difference  = (n1n2)/n1 = (1.4741.453)/1.474 = 0.01425. Modal dispersion for 1 km is
intermode = Ln1D2/[(20)(31/2)c] = 2.910-11 s 1 or 0.029 ns.
The material dispersion is
Dt1/2 = LDm D1/2 = (1 km)(7.5 ps nm-1 km-1)(3 nm) = 0.0225 ns
Assuming a Gaussian output light pulse shape,
intramode = 0.4251/2 = (0.425)(0.0225 ns) = 0.0096 ns
Total dispersion is
B = 0.25/rms = 8.2 Gb
Assume L = 1 km

## Slide 112
GRIN Rod Lenses
Point O is on the rod face center and the lens focuses the rays onto O' on to the center of the opposite face.
One pitch (P) is a full one period variation in the ray trajectory along the rod axis.
The rays from O on the rod face center are collimated out.
O is slightly away from the rod face and the rays are collimated out.

## Slide 113
Attenuation
Attenuation = Absorption + Scattering
Attenuation coefficient  is defined as the fractional decrease in the optical power per unit distance. a is in m-1.
Pout = Pinexp(L)
The attenuation of light in a medium

## Slide 114
Attenuation in Optical Fibers
Attenuation vs. wavelength for a standard silica based fiber.

## Slide 115
Lattice Absorption (Reststrahlen Absorption)
EM Wave oscillations are coupled to lattice vibrations (phonons), vibrations of the ions in the lattice. Energy is transferred from the EM wave to these lattice vibrations.
This corresponds to “Fundamental Infrared Absorption” in glasses

## Slide 116
Rayleigh Scattering
Rayleigh scattering involves the polarization of a small dielectric particle or a region that is much smaller than the light wavelength. The field forces dipole oscillations in the particle (by polarizing it) which leads to the emission of EM waves in "many" directions so that a portion of the light energy is directed away from the incident beam.
 = isothermal compressibility (at Tf)
Tf = fictive temperature (roughly the softening temperature of glass) where the liquid structure during the cooling of the fiber is frozen to become the glass structure

## Slide 117
Example: Rayleigh scattering limit
What is the attenuation due to Rayleigh scattering at around the = 1.55 m window given that pure silica (SiO2) has the following properties: Tf = 1730°C (softening temperature); T = 710-11 m2 N-1 (at high temperatures); n = 1.4446 at 1.5 m.
Solution
We simply calculate the Rayleigh scattering attenuation using
aR = 3.27610-5 m-1 or 3.27610-2 km-1
Attenuation in dB per km is
dB = 4.34R = (4.34)(3.73510-2 km-1) = 0.142 dB km-1
This represents the lowest possible attenuation for a silica glass core fiber at 1.55 m.

## Slide 118
Attenuation in Optical Fibers
Attenuation vs. wavelength for a standard silica based fiber.

## Slide 119
Low-water-peak fiber has no OH- peak
E-band is available for communications with this fiber

## Slide 120
Attenuation in Optical Fibers

## Slide 121: Attenuation
AR in dB km-1 m4
l in m
aR in dB km-1

## Slide 122: Attenuation
Glass | AR dB km-1 m4 | Comment | Glass
Silica fiber | 0.90 | "Rule of thumb" | Silica fiber
SiO2-GeO2 core step index fiber | 0.63 + 2.06×NA | NA depends on (n12 – n22)1/2 and hence on the doping difference. | SiO2-GeO2 core step index fiber
SiO2-GeO2 core graded index fiber | 0.63 + 1.75×NA |  | SiO2-GeO2 core graded index fiber
Silica, SiO2 | 0.63 | Measured on preforms. Depends on annealing. AR(Silica) = 0.59 dB km-1 mm4 for annealed. | Silica, SiO2
65%SiO235%GeO2 | 0.75 | On a preform. AR/AR(silica) = 1.19 | 65%SiO235%GeO2
(SiO2)1-x(GeO2)x | AR(silica)×(1 + 0.62x) | x = [GeO2] = Concentration as a fraction (10% GeO2, x = 0.1). For preform. | (SiO2)1-x(GeO2)x
Approximate attenuation coefficients for silica-based fibers for use in Equations (7) and (8). Square brackets represent concentration as a fraction. NA = Numerical Aperture. AR = 0.59 used as reference for pure silica, and represents AR(silica). Data mainly from K. Tsujikawa et al, Electron. Letts., 30, 351, 1994; Opt. Fib. Technol. 11, 319, 2005, H. Hughes, Telecommunications Cables (John Wiley and Sons, 1999, and references therein.)

## Slide 123: Rayleigh Scattering
Example: Consider a single mode step index fiber, which has a numerical aperture of 0.14. Predict the expected attenuation at 1.55 mm, and compare your calculation with the reported (measured) value of 0.19 - 0.20 dB km-1 for this fiber. Repeat the calculations at 1.31 µm, and compare your values with the reported 0.33 - 0.35 dB km-1 values.
Solution
First, we should check the fundamental infrared absorption at 1550 nm.
= 0.020 dB km-1, very small

## Slide 124: Rayleigh Scattering
Solution
Rayleigh scattering at 1550 nm, the simplest equation with AR = 0.9 dB km-1 mm4, gives
aR = AR/l4 = (0.90 dB km-1 mm4)/(1.55 mm)4 = 0.178 dB km-1
This equation is basically a rule of thumb. The total attenuation is then
aR + aFIR = 0.178 + 0.02 = 0.198 dB km-1.
The current fiber has NA = 0.14.
 AR = 0.63 + 2.06×NA = 0.63 + 2.06×0.14 = 0.918 dB km-1 mm4
i.e. aR = AR/l4 = (0.918 dB km-1 mm4)/(1.55 mm)4 = 0.159 dB km-1,
which gives a total attenuation of 0.159 + 0.020 or 0.179 dB km-1.

## Slide 125
Solution
We can repeat the above calculations at l = 1.31 mm. However, we do not need to add aFIR.
aR = AR/l4 = (0.90 dB km-1 mm4)/(1.31 mm)4 = 0.306 dB km-1
and using the NA based for AR,
aR = AR/l4 = (0.918 dB km-1 mm4)/(1.31 mm)4 = 0.312 dB km-1.
Both close to the measured value.
Rayleigh Scattering

## Slide 126: Bending Loss
Definitions of (a) microbending and (b) macrobending loss and the definition of the radius of curvature, R. (A schematic illustration only.) The propagating mode in the fiber is shown as white painted area. Some radiation is lost in the region where the fiber is bent. D is the fiber diameter, including the cladding.

## Slide 127: Bending Loss
Microbending loss
the radius of curvature R of the bend is sharp
bend radius is comparable to the diameter of the fiber
Typically microbending losses are significant when the radius of curvature of the bend is less than 0.1 - 1 mm.
They can arise from careless or poor cabling of the fiber or even in flaws in manufacturing that result in variations in the fiber geometry over small distances.

## Slide 128: Bending Loss
Macrobending losses
Losses that arise when the bend is much larger than the fiber size
Typically much grater than 1 mm
Typically occur when the fiber is bent during the installation of a fiber optic link such as turning the fiber around a corner.
There is no simple precise and sharp boundary line between microbending and macrobending loss definitions.
Both losses essentially result from changes in the waveguide geometry and properties as the fiber is subjected to external forces that bend the fiber.
Typically, macrobending loss crosses over into microbending loss when the radius of curvature becomes less than a few millimeters.

## Slide 129
Bending Loss
Sharp bends change the local waveguide geometry that can lead to waves escaping. The zigzagging ray suddenly finds itself with an incidence angle smaller than q that gives rise to either a transmitted wave, or to a greater cladding penetration; the field reaches the outside medium and some light energy is lost.

## Slide 130
Bending Loss
When a fiber is bent sharply, the propagating wavefront along the straight fiber cannot bend around and continue as a wavefront because a portion of it (black shaded) beyond the critical radial distance rc must travel faster than the speed of light in vacuum. This portion is lost in the cladding- radiated away.

## Slide 131
Bending Loss
(a) Bending loss in dB per turn of fiber for three types of fibers, standard single mode, and two trench fibers, around 1.55 - 1.65 mm. (b) The index profile for the trench fiber 1 in (a), and a schematic view of the fiber cross section. Experimental data have been used to generate the plots have been combined from various sources. (Standard fiber, M.-J. Li et al. J. Light Wave Technol., 27, 376, 2009; trench fiber 1, K. Himeno et al, J. Light Wave Technol., 23, 3494, 2005, trench fiber 2, L.-A. de Montmorillon, et al. “Bend-Optimized G.652D Compatible Trench-Assisted Single-Mode Fibers”, Proceedings of the 55th IWCS/Focus, pp. 342-347, November, 2006.)

## Slide 132: Bend Insensitive Fibers
Left, the basic structure of bend insensitive fiber with a nanoengineered ring in the cladding. Right, an SEM picture of the cross section of a nanoengineered fiber with reduced bending losses. (Courtesy of Ming-Jun Li, Corning Inc. For more information see US Patent 8,055.110, 2011)

## Slide 133: Bending Loss in Fibers General Description
aB = Aexp(-R/Rc)
A and Rc are constants

## Slide 134
Bending Loss
aB = Aexp(-R/Rc)
where A and Rc are constants
For single mode fibers, a quantity called a MAC-value, or a MAC-number, NMAC, has been used to characterize the bending loss. NMAC is defined by

## Slide 135
Microbending Loss
Measured microbending loss for a 10 cm fiber bent by different amounts of radius of curvature R. Single mode fiber with a core diameter of 3.9 mm, cladding radius 48 mm, D = 0.00275, NA  0.10, V  1.67 and 2.08. Data extracted from A.J. Harris and P.F. Castle, "Bend Loss Measurements on High Aperture Single-Mode Fibers as a Function of Wavelength and Bend Radius", IEEE J. Light Wave Technology, Vol. LT14, 34, 1986, and repotted with a smoothed curve; see original article for the discussion of peaks in aB vs. R at 790 nm).

## Slide 136: Bending Loss in SMF
aB = Aexp(-R/Rc)
MAC-value, or a MAC-number, NMAC
NOTES
aB increases with increasing MFD
aB decreasing cut-off wavelength.
aB increases exponentially with the MAC-number
It is not a universal function, and different types of fibers, with very different refractive index profiles, can exhibit different aB-NMAC behavior.
NMAC values are typically in the range 6 - 8

## Slide 137: Standard Fibers and Bending Loss
aB = Aexp(-R/Rc)
OM1 MMF for use at 850 and 1310
OM1
“Maximum bending (macrobending) loss of 0.5 dB when the fiber is wound 100 turns with a radius 75 mm i.e. a bending loss of 0.005 dB/turn for a bend radius of 75 mm.”
Bend insensitive fibers have been designed to have lower bend losses. For example, some fiber manufacturers specify the allowed bend radius for a given level of attenuation at a certain wavelength (e.g. 1310 nm)

## Slide 138
Example: Experiments on a standard SMF operating around 1550 nm have shown that the bending loss is 0.124 dB/turn when the bend radius is 12.5 mm and 15.0 dB/turn when the bend radius is 5.0 mm. What is the loss at a bend radius of 10 mm?
Bending Loss Example
Solution
Apply
aB = Aexp(-R/Rc)
0.124 dB/turn = Aexp[-(12.5 mm)/Rc]
15.0 dB/turn = Aexp[-(5.0 mm)/Rc]
Solve for A and Rc. Dividing the first by the second and separating out Rc we find,
Rc = (12.5 mm - 5.0 mm) / ln(15.0/0.124) = 1.56 mm
and A = (15.0 dB/turn) exp[(5.0 mm)/(1.56 mm] = 370 dB/turn
At R = 10 mm
aB = Aexp(-R/Rc) = (370)exp[-(10 mm)/(1.56 mm)]
= 0.61 dB/turn.
The experimental value is also 0.61 dB/turn to within two decimals.

## Slide 139
Example: Microbending loss It is found that for a single mode fiber with a cut-off wavelength c = 1180 nm, operating at 1300 nm, the microbending loss reaches 1 dB m-1 when the radius of curvature of the bend is roughly 6 mm for  = 0.00825, 12 mm for  = 0.00550 and 35 mm for  = 0.00275. Explain these findings.
Solution:
Given  = 1, R increases from R1 to R2 when V decreases from V1 to V2.
ExpectedR with V
Equivalently at one R = R1,  with V
We can generalize by noting that the penetration depth into the cladding  1/V.
ExpectedR with 
Equivalently at one R = R1,  with 
Thus, microbending loss  gets worse when penetration  into cladding increases; intuitively correct. Experiments show that for a given  = 1, R increases with decreasing . We know from basic optics  with i.e. increases with decreasing .
Thus expected R with  with  as observed

## Slide 140
Example: Microbending loss It is found that for a single mode fiber with a cut-off wavelength c = 1180 nm, operating at 1300 nm, the microbending loss reaches 1 dB m-1 when the radius of curvature of the bend is roughly 6 mm for  = 0.00825, 12 mm for  = 0.00550 and 35 mm for  = 0.00275. Explain these findings.
Solution:
Rc is a constant (“a critical radius type of constant”) that is proportional to . Taking logs,
lna = -D3/2R + constant
We are interested in the vs R behavior at a constant . We can lump the constant into ln and obtain,
 R-2/3
The plot in the figure gives an index close this value.

## Slide 141
Manufacture of Optical Fibers

## Slide 142
The cross section of a typical single-mode fiber with a tight buffer tube. (d = diameter)
Typical Cross Section of an Optical Fiber

## Slide 143
Outside vapor Deposition (OVD)
Main reactions are
Silicon tetrachloride and oxygen produces silica
SiCl4(gas) + O2(gas)  SiO2(solid) + 2Cl2(gas)
Germanium tetrachloride and oxygen produces germania
GeCl4(gas) + O2(gas)  GeO2(solid) + 2Cl2(gas)

## Slide 144
Donald Keck, Bob Maurer and Peter Schultz (left to right) at Corning shortly after announcing the first low loss optical fibers made in 1970. Keck, Maurer and Schultz developed the outside vapor deposition (OVD) method for the fabrication of preforms that are used in drawing fibers with low losses. Their OVD was based on Franklin Hyde’s vapor deposition process earlier at Corning in 1930s. OVD is still used today at Corning in manufacturing low loss fibers. (Courtesy of Corning)

## Slide 145
Peter Schultz making a germania-doped multimode fiber preform using the outside vapor deposition (OVD) process circa 1972 at Corning. Soot is deposited layer by layer on a thin bait rod rotating and translating in front of the flame hydrolysis burner. The first fibers made by the OVD at that time had an attenuation of 4 dB/km, which was among the lowest, and below what Charles Kao thought was needed for optical fiber communications, 20 dB/km (Courtesy of Peter Schultz.)

## Slide 146
Outside Vapor Deposition (OVD)
Schematic illustration of OVD and the preform preparation for fiber drawing. (a) Reaction of gases in the burner flame produces glass soot that deposits on to the outside surface of the mandrel. (b) The mandrel is removed and the hollow porous soot preform is consolidated; the soot particles are sintered, fused, together to form a clear glass rod. (c) The consolidated glass rod is used as a preform in fiber drawing.

## Slide 147: WAVELENGTH DIVISION MULTIPLEXING: WDM

## Slide 148: WAVELENGTH DIVISION MULTIPLEXING: WDM
Generation of different wavelengths of light each with a narrow spectrum to avoid any overlap in wavelengths.
Modulation of light without wavelength distortion; i.e. without chirping (variation in the frequency of light due to modulation).
Efficient coupling of different wavelengths into a single transmission medium.
Optical amplification of all the wavelengths by an amount that compensates for attenuation in the transmission medium, which depends on the wavelength.
Dropping and adding channels when necessary during transmission.
Demultiplexing the wavelengths into individual channels at the receiving end.
Detecting the signal in each channel. To achieve an acceptable bandwidth, we need to dispersion manage the fiber (use dispersion compensation fibers), and to reduce cross-talk and unwanted signals, we have to use optical filters to block or pass the required wavelengths. We need various optical components to connect the devices together and implement the whole system.

## Slide 149: WAVELENGTH DIVISION MULTIPLEXING: WDM
If Du < 200 GHz then WDM is called dense wavelength division multiplexing and denoted as DWDM.
At present, DWDM stands typically at 100 GHz separated channels which is equivalent to a wavelength separation of 0.8 nm.
DWDM imposes stringent requirements on lasers and modulators used for generating the optical signals.
It is not possible to tolerate even slight shifts in the optical signal frequency when channels are spaced closely. As the channel spacing becomes narrower as in DWDM, one also encounters various other problems not previously present. For example, any nonlinearity in a component carrying the channels can produce intermodulation between the channels; an undesirable effect. Thus, the total optical power must be kept below the onset of nonlinearity in the fiber and optical amplifiers within the WDM system.

## Slide 150: Nonlinear Effects and DWDM
Induced Polarization, P = a1E + a2E2 + a3E3
P = a1E + a3E3
Nonlinear behavior for glasses
Nonlinear effects
Consider signals at 3 channels
E1 = C1cos(2pu1t) E2 = C2cos(2pu2t) E3 = C3cos(2pu3t)
Nonlinear P = a3E3 = a3(E1 + E2 + E3)3
= a3(E13) + …+ 2a3(E1E2E3) +...+ a3(E33)
Four photon mixing

## Slide 151: Nonlinear Effects and DWDM
Nonlinear P = a3(E13) +…+ 2a3(E1E2E3) +...+ a3(E33)
Nonlinear P = …+ 2a3C1C2C3cos(2pu1t)cos(2pu2t)cos(2pu3t) +…
Frequencies mix and can be written as sum and difference frequencies
Consider three optical signals at
1
2 = 1 +GHz 
3 = 2 +GHz  = 1 +200 GHz

## Slide 152: Nonlinear Effects and DWDM Four Photon (Wave) Mixing
Three photons (1 2 3 ) mix to generate a fourth photon (4 )
4 = 1 + 2 - 3
4 = 1 + 1 +GHz  1 +200 GHz
4 = 1 GHz on top of previous channel

## Slide 153: Nonlinear Effects: Frequency Chirping
n = no + n2I
Nonlinear refractive index
Self-phase modulation
Frequency chirping

## Slide 154: Nonlinear Effects: Frequency Chirping
n = no + n2I
Self-phase modulation
Frequency chirping

## Slide 155: Stimulated Brillouin Scattering
(a) Scattering of a forward travelling EM wave A by an acoustic wave results in a reflected, backscattered, wave B that has a slightly different frequency, by W. (b) The forward and reflected waves, A and B respectively, interfere to give rise to a standing wave that propagates at the acoustic velocity va. As a result of electrostriction, an acoustic wave is generated that reinforces the original acoustic wave and stimulates further scattering.

## Slide 156: Stimulated Brillouin Scattering (SBS)
Atomic vibrations give rise to traveling waves in the bulk  phonons. Collective vibrations of the atoms in a solid give rise to lattice waves inside the solid
Acoustic lattice waves in a solid involve periodic strain variations along the direction of propagation.
Changes in the strain result in changes in the refractive index through a phenomenon called the photoelastic effect. (The refractive index depends on strain.) Thus, there is a periodic variation in the refractive index which moves with an acoustic velocity va as depicted
The moving diffraction grating reflects back some of the forward propagating EM wave A to give rise to a back scattered wave B as shown. The frequency wB of the back scattered wave B is Doppler shifted from that of the forward wave wA by the frequency W of the acoustic wave i.e. wB = wA - W.

## Slide 157: Stimulated Brillouin Scattering (SBS)
The forward wave A and the back scattered wave B interfere and give rise to a standing wave C.
This standing wave C represents a periodic variation in the field that moves with a velocity va along the direction of the original acoustic wave
The field variation in C produces a periodic displacement of the atoms in the medium, through a phenomenon called electrostriction. (The application of an electric field causes a substance to change shape, i.e. experience strain.). Therefore, a periodic variation in strain develops, which moves at the acoustic velocity va.
The moving strain variation is really an acoustic wave, which reinforces the original acoustic wave and stimulates more back scattering. Thus, it is clear that, a condition can be easily reached that Brillouin scattering stimulates further scattering; stimulated Brillouin scattering (SBS).

## Slide 158: Stimulated Brillouin Scattering (SBS)
The SBS effect increases as the input light power increase
The SBS effect increases as the spectral width of the input light becomes narrower.
The onset of SBS depends not only on the fiber type and core diameter, but also on the spectral width Dl of the laser output spectrum.
SBS is enhanced as the laser spectral width Dl is narrowed or the duration of light pulse is lengthened.
Typical values: For a directly modulated laser diode emitting at 1550 nm into a single mode fiber, the onset of SBS is expected to occur at power levels greater than 20 - 30 mW. In DWDM systems with externally modulated lasers, i.e. narrower Dl, the onset of SBS can be as low as ~10 mW. SBS is an important limiting factor in transmitting high power signals in WDM systems.

## Slide 159: Bragg Fibers
The high (n1) and low (n2) alternating refractive index profile constitutes a Bragg grating which acts as a dielectric mirror.
There is a band of wavelengths, forming a stop-band, that are not allowed to propagate into the Bragg grating.
We can also view the periodic variation in n as forming a photonic crystal cladding in one-dimension, along the radial direction, with a stop-band, i.e. a photonic bandgap.
Light is bound within the core of the guide for wavelengths within this stop-band. Light can only propagate along z. The cladding is like a dielectric mirror
d1 = l/4n1 and d2 = l/4n2
Bragg fibers have a core region surrounded by a cladding that is made up of concentrating layers of high low refractive index dielectric media
The core can be a low refractive index solid material or simply hollow. In the latter case, we have a hollow Bragg fiber.

d1n1 = d2n2
Corrected

## Slide 160: Bragg Fibers
Bragg reflections from the cladding need
2  (kn1d1 + kn2d2) = m(2p)
(2p/l)2(n1d1 + n2d2) = m(2p)

n1d1 + n2d2 = m(l/2)
This is satisfied for d1 = l/4n1 and d2 = l/4n2
d1n1 = d2n2

Integer
Behaves like a dielectric mirror
Layers are quarter wavelength thick

## Slide 161: Bragg Fibers
(a) A Bragg fiber and its cross section. The Bragg grating in the cladding can be viewed to reflect the waves back into the core over its stop-band. (b) The refractive index variation (exaggerated). (c) Typical field distribution for the circumferential field Eq.

## Slide 162: Photonic Crystal Fibers: Holey Fibers
(a) A solid core PCF. Light is index guided. The cladding has a hexagonal array of holes. d is the hole diameter and L is the array pitch, spacing between the holes (b) and (c) A hollow core PCF. Light is photonic bandgap (PBG) guided.

## Slide 163: Photonic Crystal Fibers: Holey Fibers
Left: The first solid core photonic crystal fiber prepared by Philip Russell and coworkers at the University of Bath in 1996; an endlessly single mode fiber. (Courtesy of Philip Russell)
Left: One of the first hollow core photonic crystal fibers, guiding light by the photonic bandgap effect (1998) (Courtesy of Philip Russell)
Above: A commercially available hollow core photonic crystal fiber from Blaze Photonics. (Courtesy of Philip Russell)

## Slide 164: Photonic Crystal Fibers: Holey Fibers
Philip Russell (center), currently at the Max Planck Institute for the Science of Light in Erlangen, Germany, led the team of two postdoctoral research fellows, Jonathan Knight (left) and Tim Birks (right) (both currently professors at the University of Bath in England) that carried out the initial pioneering research on photonic crystal fibers in the 1990s. (See reviews by P.St.J. Russell, Science, 299, 358, 2003, J. C. Knight, Nature, 424, 847, 2003) (Courtesy of Philip Russell)

## Slide 165: Solid Core Photonic Crystal Fibers
Both the core and cladding use the same material, usually silica, but the air holes in the cladding result in an effective refractive index that is lower than the solid core region.
The cladding has a lower effective refractive index than the core, and the whole structure then is like a step index fiber.
Total internal reflection then allows the light to be propagated just as in a step index standard silica fiber. Light is index guided.

## Slide 166: Solid Core Photonic Crystal Fibers
The solid can be pure silica, rather than germania-doped silica, and hence exhibits lower scattering loss.
Single mode propagation can occur over a very large range of wavelengths, almost as if the fiber is endlessly single mode (ESM). The reason is that the PC in the cladding acts as a filter in the transverse direction, which allows the higher modes to escape (leak out) but not the fundamental mode.
(a) The fundamental mode is confined. (b) Higher modes have more nodes and can leak away through the space.

## Slide 167: Solid Core Photonic Crystal Fibers
ESM operation: The core of a PCF can be made quite large without losing the single mode operation. The refractive index difference can also be made large by having holes in the cladding. Consequently, PCFs can have high numerical apertures and large core areas; thus, more light can be launched into a PCF. Further, the manipulation of the shape and size of the hole, and the type of lattice (and hence the periodicity i.e. the lattice pitch) leads to a much greater control of chromatic dispersion.
(a) The fundamental mode is confined. (b) Higher modes have more nodes and can leak away through the space.

## Slide 168: Hollow Core Photonic Crystal Fibers: Holey Fibers
Notice that the core has a lower refractive index (it is hollow) so that we cannot rely on total internal reflection (TIR) to explain light propagation.
Light in the transverse direction is reflected back into the core over frequencies within the stop-band, i.e. photonic bandgap (PBG), of the photonic crystal in the cladding. When light is launched from one end of the fiber, it cannot enter the cladding (its frequency is within the stop-band) and is therefore confined within the hollow core. Light is photonic bandgap guided.

## Slide 169: Hollow Core Photonic Crystal Fibers: Holey Fibers
As recalled by Philip Russell:
"My idea, then, was to trap light in a hollow core by means of a 2D photonic crystal of microscopic air capillaries running along the entire length of a glass fiber. Appropriately designed, this array would support a PBG for incidence from air, preventing the escape of light from a hollow core into the photonic-crystal cladding and avoiding the need for TIR." (P. St.J. Russell, J. Light Wave Technol, 24, 4729, 2006)
The periodic arrangement of the air holes in the cladding creates a photonic bandgap in the transverse direction that confines the light to the hollow core.

## Slide 170: Hollow Core Photonic Crystal Fibers: Holey Fibers
There are certain distinct advantages
Material dispersion is absent.
The attenuation in principle should be potentially very small since there is no Rayleigh scattering in the core. However, scattering from irregularities in the air-cladding interface, that is, surface roughness, seems to limit the attenuation.
High powers of light can be launched without having nonlinear effects such as stimulated Brillouin scattering limiting the propagation.
There are other distinct advantages that are related to strong nonlinear effects, which are associated with the photonic crystal cladding.

## Slide 171: Fiber Bragg Gratings and FBG Sensors
Fiber Bragg Grating (FBG) based optical strain sensor for monitoring strains in civil structures e.g. bridges, dams, buildings, tunnels and building. The fiber is mounted on a steel carrier and maintained stretched. The carriage is welded to the steel structure. (Courtesy of Micron Optics)
Fiber Bragg Grating (FBG) based optical temperature sensors for use from -200 C to 250 C. FBGs are mounted in different packages: top, left, all dielectric, top right, stainless steel and bottom, copper. The sensors operate over 1510 - 1590 nm. (Courtesy of Lake Shore Cryotronics Inc.)

## Slide 172: FBG: Fiber Bragg Grating
Fiber Bragg grating has a Bragg grating written in the core of a single mode fiber over a certain length of the fiber. The Bragg grating reflects any light that has the Bragg wavelength lB, which depends on the refractive index and the periodicity. The transmitted spectrum has the Bragg wavelength missing.

## Slide 173: Fiber Bragg Grating: FBG
Variation in n in the grating acts like a dielectric mirror
Partial Fresnel reflections from the changes in the refractive index add in phase and give rise to a back reflected (back diffracted) wave only at a certain wavelength lB, called the Bragg wavelength
Integer, 1,2,… normally q = 1 is used, the fundamental

## Slide 174: Bragg Wavelength lB
A
B
L
Repeat unit = unit cell
For reflection A and B must be in phase i.e. phase difference should be q2p. This will be so at wavelength lB, the Bragg wavelength. The phase difference between A and B is DFAB
A and B are reflected waves
Average index in unit cell

## Slide 175: Fiber Bragg Grating: FBG
kL < 1 Weak
kL > 1 Strong
Reflectance, R

## Slide 176: FBG Sensors
Photoelastic or elasto-optic coefficient
Strain

## Slide 177: FBG Sensors
Consider strain which results in changes in n and L

## Slide 178: FBG Sensors
A highly simplified schematic diagram of a multiplexed Bragg grating based sensing system. The FBG sensors are distributed on a single fiber that is embedded in the structure in which strains are to be monitored. The coupler allows optical power to be coupled from one fiber to the other.

## Slide 179: FBG at 1550 nm
EXAMPLE
A silica fiber based FBG is required to operate at 1550 nm. What should be the periodicity of the grating L? If the amplitude of index variation Dn is 10-4 and total length of the FBG is 10 mm, what is the reflectance at the Bragg wavelength and the spectral width of the reflected light? Assume that the effective refractive index is 1.4550
We can use
1550 nm = 2(1.450)(L) so that the grating periodicity L = 534.5 nm
The coupling coefficient k is by
k = pDn/l = p(10-4)/(1550×10-9 m) = 202.7 m-1.
Thus, kL = 2.027, so the FBG is a strong grating. The reflectance is
SOLUTION
= tanh2(2.027) = 0.933 or 93.3%
= 0.428 nm
The reflectance and spectral width values are approximate inasmuch as above equations contain a number of assumptions.

## Slide 180: Appendix I: FBG Strain Gauge
or

Some researchers use
and
Compare with (2.15.7)
What is the difference?

## Slide 181: Appendix I
compare with
For silica glass, take n  1.44


## Slide 182
Updates and
Corrected Slides
Class Demonstrations
Class Problems
Check author’s website
http://optoelectronics.usask.ca
Email errors and corrections to safa.kasap@yahoo.com